 
	Extrusion Line:
	8 extrusion lines and Oxidation line, daily output can reach 20000sets.

	Production Line:
	5 production line for CNC

	Product Capacity:
	Anodizing Electrophoresis monthly output is 2000 tons.

	
	Powder Coating monthly output is 2000 tons.

	
	Wood Grain monthly output is 1000 tons.

	Alloy:
	6063/6061/6005/6060/7005. (Special alloy could be made upon your requirements.)

	Temper :
	T3-T8

	Standard:
	China GB high precision standard.

	Thickness:
	Based on your requirements.

	Length:
	3-6 M or customized length. And we can produce any length you want.

	MOQ:
	Normally 2 tons. Usually 15-17 tons for 1*20GP and 23-27 tons for 1*40HQ.

	Surface Finish:
	Mill finish, Anodizing, Powder coating, Wood grain, Polishing, Brushing, Electrophoresis.

	Color We Can Do:
	Silver, black, white, bronze, champagne, green, gray, golden yellow, nickel, or customized.

	Film Thickness:
	Anodized:
	Customized. Normal thickness: 8 um-25um.

	
	Powder Coating:
	Customized. Normal thickness: 60-120 um.

	
	Electrophoresis Complex Film:
	Normal thickness: 15 um.

	Chemical Composition & Performance:
	Meet and execution by the China GB high precision level.

	Machining:
	Cutting, punching, drilling, bending, weld, mill, CNC, etc.

	Packing:
	Plastic film & Kraft paper. Protect film for each piece of profile is also ok if required.


